# Model Parameters, Assumptions and Deviations

# Approach

Langmuir isotherm (spec Section 2) fitted to Langmi et al. (2003) zeolite 5A data at 77 K, transferred to the operating temperature through the affinity constant b(T) = b(77 K) × exp[(q_st/R)(1/T − 1/77)]. Saturation capacity counts adsorption sites and is held temperature-independent. The vessel is a lumped, well-mixed tank (Section 6) with ideal-gas behaviour (Section 5) and instantaneous adsorption equilibrium (Section 5).

# Fitted parameters

| Quantity | Value | Source |
| --- | --- | --- |
| q_max (5A basis) | 1.2260 wt% | Fitted to Langmi (2003) |
| b at 77 K | 0.3169 /bar | Fitted to Langmi (2003) |
| Fit max error | 7.81% | Langmuir, 5 points |
| Powder enhancement | ×1.15 | Erdogan et al. (2024) |
| Granule binder fraction | 0.175 | Sister spec; not given here |
| Regular-form factor | ×0.75 | ESTIMATE — see below |

# Deviations and flagged assumptions

## The 2.2 wt% plausibility floor is a 77 K figure [SPEC-DEV-1]

Section 2's developer note cites '~2.2 wt% at near-ambient temperature, 0–15 bar' and instructs treating it as a floor to exceed at −78 °C. Zeolites hold on the order of 1e-3 wt% at 25 °C and ~0.05 wt% at −78 °C; 2.2 wt% is a liquid-nitrogen result. Anchoring to it would embed a 40–1000× error. It is recorded here as a citation to correct before submission.

## Isothermal and thermal-swing cannot both hold [SPEC-DEV-2]

Section 5 fixes the model isothermal at −78 °C; Section 4 desorbs by heating to 80–100 °C. Modelled as isothermal within each stage with explicit ramps between.

## Source pressure cannot fill to target [SPEC-DEV-3]

Section 4 gives a source 'below 10 bar' and a target of 10 bar. Source pressure is a parameter defaulting above the target so charging can complete.

## 'Zeolite-14A' is not a standard designation [SPEC-DEV-4]

LTA is supplied as 3A/4A/5A; 13X is a FAU framework. Ca-exchanged zeolite A is 5A and untreated Na-form zeolite A is 4A. The activated/regular pair is modelled as 5A/4A — which means published isotherms already exist for the activated samples.

## No adsorption kinetics exist in this model [SPEC-DEV-5]

Section 5 specifies instantaneous equilibrium, so the sorbent contributes no time constant. The 'desorption vs time' curve required by Section 7 is shaped entirely by the heating and venting schedule.

## Regular-form capacity is an unanchored estimate

Regular (Na-form, 4A) capacity is estimated at 75% of the Ca-exchanged (5A) value. No published 4A isotherm is supplied by the specification. This single number sets the entire activated-vs-regular result and must be replaced with a measured or literature isotherm before the comparison carries any weight.

## Heating assumed to occur with the outlet closed

The specification does not say whether the vessel is sealed during the heating stage. Sealed is modelled as the conservative case, and it is what produces the over-pressure finding. If the outlet is open to the delivery line throughout heating, peak pressure stays at the delivery value and the finding does not apply.

## Insulation not specified

Section 3 notes insulation is present but gives no type or thickness. The isothermal assumption stands in for perfect insulation; no heat-leak term is modelled, so hold-time performance is optimistic.