# Hydrogen Storage Vessel Simulation — Results

Generated against 'H2 Zeolite Vessel Simulation Spec.docx'. Predictive simulation; no physical H₂ testing was performed.

# 1. Adsorption Isotherms

Equilibrium capacity at -78 °C for each of the four samples, Langmuir model with q_st = 6 kJ/mol.

| # | Sample | q_max (wt%) | 1 bar | 5 bar | 10 bar |
| --- | --- | --- | --- | --- | --- |
| 1 | Ca-activated powder (5A (CaA)) | 1.4098 | 0.00153 | 0.00763 | 0.01517 |
| 2 | Regular powder (4A (NaA)) | 1.0574 | 0.00115 | 0.00572 | 0.01138 |
| 3 | Ca-activated granule (5A (CaA)) | 1.0114 | 0.00110 | 0.00547 | 0.01088 |
| 4 | Regular granule (4A (NaA)) | 0.7586 | 0.00082 | 0.00410 | 0.00816 |

# 2. Duty Cycle Performance

| # | Sample | Charged (g) | Working (g) | Peak P (bar) | % of DOE |
| --- | --- | --- | --- | --- | --- |
| 1 | Ca-activated powder | 0.01896 | 0.01862 | 19.12 | 0.276% |
| 2 | Regular powder | 0.01422 | 0.01396 | 19.00 | 0.207% |
| 3 | Ca-activated granule | 0.01361 | 0.01336 | 18.96 | 0.198% |
| 4 | Regular granule | 0.01020 | 0.01002 | 18.87 | 0.148% |

# 3. Findings the Specification Does Not Anticipate

## Peak pressure exceeds the vessel design rating

Heating a sealed vessel from -78 °C to 90 °C at 10 bar raises pressure to 19.1 bar, against the 15 bar design rating in Section 3. Gas-law expansion alone accounts for most of it; desorbed hydrogen adds the rest. Either the outlet must be open during heating, the charge pressure reduced, or the rating raised. This is a safety item, not a modelling artefact.

## Storage is dominated by compressed gas, not adsorption

At the charged state the best sample holds 0.0190 g by adsorption against 0.4481 g as free gas in the void volume — adsorption contributes only 4.1%. The sorbent is not doing the storage work at this temperature.

## Distance from the DOE target

The best sample reaches 0.0152 wt%, which is 0.28% of the 5.5 wt% target named in Section 1. This is the expected result for physisorption above 77 K and should be stated directly rather than presented as a shortfall to explain away.

## Cycles are identical by construction

No degradation mechanism is specified. With instantaneous equilibrium and no fade term, all five cycles return exactly the same numbers. The capacity-vs-cycle plot is therefore flat by definition and demonstrates nothing about durability. A measured or literature fade rate is needed before that plot carries meaning.